General  Plating

TABLE- 1 (Tin-Plated)

| Plating Code | Top Plating Thickness | Under Plating Thickness | Area | Match Type |
| --- | --- | --- | --- | --- |
| 1 | 30μ” Tin Min. | Reflow Plated | Overall | Crimp clip terminal |
|  | 80μ” Tin Min. | 30μ”Nickel Min. | Overall | Crimp clip terminal |
|  | 100μ” Tin Min. | 30μ Nickel Min. | Overall | Solder tail terminal & Board in terminal |
|  | 120μ” Tin Min. | 30μ Nickel Min. | Overall | Square or round pin |
|  | 120μ” Tin | 50μ Nickel Min. | Overall | SMT type terminal |

TABLE- 2 (Gold -Plated)

| Plating Code | Top Plating Thickness | Under Plating Thickness | Area | Match Type |
| --- | --- | --- | --- | --- |
| 2 | 0.8μ” Gold Min. | 50μ” Nickel Min. | Overall | Square or round pin |
|  | 1.2μ” Gold Min. |  |  | Other type |
| 3 | 15μ” Gold Min. | 50μ” Nickel | Overall | All type |
| 4 | 30μ” Gold Min. | 50μ” Nickel | Overall | All type |
| 5 | 50μ” Gold Min. | 50μ” Nickel | Overall | All type |
| 7 | 3μ” Gold Min. | 50μ” Nickel | Overall | All type |
| 8 | 80μ” Gold Plated over | 50μ” Nickel | Overall | CP35 |
| 9 | 5μ” Gold Plated over | 50μ” Nickel | Overall | All type |
| A | Selective 1.2μ” Gold Flash | 50μ” Nickel | Contact Area | All type |
| B | Selective 15μ” Gold | 50μ” Nickel | Contact Area | All type |
| C | Selective 30μ” Gold | 50μ” Nickel | Contact Area | All type |

General  Plating

| D | Selective 10μ” Gold | 50μ” Nickel | Contact Area | All type |
| --- | --- | --- | --- | --- |
| E | Selective 50μ” Gold | 50μ” Nickel | Contact Area | All type |
| F | Selective 80μ” Gold | 50μ” Nickel | Contact Area | CP35 |
| G | Selective 5μ” Gold | 50μ” Nickel | Contact Area | CCF |
| I | Selective 15μ” Gold | 1.2μ” Gold Flash Plated over 50μ” Nickel | Contact Area | All type |
| J | Selective 30μ” Gold | 1.2μ” Gold Flash Plated over 50μ” Nickel | Contact Area | All type |
| K | Selective 5μ” Gold | 80μ” Nickel | Contact Area | All type |

SOLDERABILITY:

| TEST ITEM | TEST CONDITION | PROCESS | TEST REQUIREMENT |
| --- | --- | --- | --- |
| Solder ability | Soldering time: 5±0.5 Second Soldering pot: 230±5℃ | Sn - Pb Process | Minimum: 95( of immersed area |
|  | Soldering time: 3±0.5 Second Soldering pot: 245±5℃ | Lead Free Process |  |